## Slide 1: Analysis of tensile properties in a prepreg platelet molded composite system
Sergey Kravchenko, PhD
Postdoctoral Researcher
Composites Manufacturing & Simulation Center
Purdue University

## Slide 2: Performance Analysis & Understanding of structure-property relationship
Structure
Properties
Performance
Processing
Analysis
Experimental
Theoretical
Computational Damage Mechanics
Lp
wp
tp
1
2
x1
x2
x3

## Slide 3: Hierarchical subordination in a prepreg molded composite system
Individual platelets
A-A
Semi-laminated structure of a platelet-stacked composite system
1 mm
100 μm
Individual
fibers
20 μm
Macro-scale
Meso-scale
Micro-scale
Macro-scale effective properties
Complex meso-scale interactions between large number of platelets
Composite meso-structure

## Slide 4: Meso-structure descriptors & characteristics

## Slide 5: Descriptors and characteristics of the platelet composite meso-structure
x1
x2
x3
Lp
wp
tp
1
2
Structure of a Composite System
Platelet Geometry
Composite Morphology
Geometrical Arrangement/ Overlapping
Orientation State
Effective
Properties & Variability
Platelets Count
Composite System
of Platelets
Complex System
Highly Redundant Structure

## Slide 6: Orientation state in a platelet composite system: stochastic or deterministic
x1
x2
x3
x1
x2
x3
Precursor CF Tape
Platelet System with
Stochastic Orientation State
Platelet System with Deterministic Orientation State
Improved
Hierarchical
Organization
of
Composite
Structure
Engineered/Semi-Controlled Morphology
Uncontrolled Irregular Morphology

## Slide 7: Implications of structure descriptors for composite performance characteristics
Orientation State
Platelets Count
Orthotropic mechanical properties of a platelet are a function of orientation
Platelet Geometry
Geometrical Arrangement/ Overlapping
Efficiency of load transfer (stress sharing)
Internal redundancy of composite system
Variability of morphology descriptors
Effective Properties
Variability
of Effective Properties

## Slide 8: Implications of structure descriptors for composite performance characteristics
Platelet Geometry
Geometrical Arrangement/ Overlapping
Efficiency of load transfer (stress sharing)
Effective Properties
Variability
of Effective Properties

## Slide 9: Stress transfer efficiency & composite system performance
Platelets support more in-plane stress & fracture
Interlaminar stresses are greater to cause disbonding
x1
x3
x2
More Efficient
Stress Transfer
Less
Efficient
x1
x3
x2
x1
x3
x2
Array of Aligned Staggered Platelets
Thinner platelets
Thicker platelets

## Slide 10: What defines stress transfer efficiency?
Improved Effective Strength of Composite System
Improved Stress Transfer by Platelet Geometry (Lp/tp ↑)
Improved Stress Transfer by Platelets Arrangement (more overlap length)
Platelet Geometry
Geometrical Arrangement
of Platelets

## Slide 11: Implications of structure descriptors for composite performance characteristics
Platelets Count
Internal redundancy of composite system
Variability of morphology descriptors
Effective Properties
Variability
of Effective Properties

## Slide 12: Two ways to vary the platelets count (stochastic & deterministic systems)
Platelets Count
by Increasing Composite System Volume
Platelets Count
by Changing Platelet Size
Volume, V1
Volume, V1
Volume, V2 > V1
Fixed Volume
Active/Direct
Passive/Indirect

## Slide 13: Implications of structure descriptors for composite performance characteristics
Orientation State
Orthotropic mechanical properties of a platelet are a function of orientation
Effective Properties

## Slide 14: Alignment of platelets is a significant feature of orientation state
Influence on
Orientation State
Active/Direct
Passive/Indirect
Stochastic system: Introduce preferential alignment
Deterministic system: Design/assign orientation state
By platelets count in a stochastic system
x1
x2
x3
x1
x2
x3
Platelets Alignment
(with the global x1-direction)

## Slide 15: Orientation tensor as an up-scale measure of orientation disorder in a system of many platelets
Degree of overall alignment
in a system of N platelets
x1
x2
x1
x2
x1
x2
x1
x2
x1
x2
a11= 1.0
a11= 0.89
a11= 0.53
a11= 0.32
a11= 0.0
A convenient large scale descriptor of the orientation state in a composite system containing a large number of misaligned platelets

## Slide 16: Domain and sub-domains: importance of local effects
Local variability of morphological features defines the overall response of composite system, both stiffness and strength
Understanding of local & global degree of alignment is important
Simple analogy is effective stiffness () of springs in series:
Spring 1
Spring 2
Spring 3
Spring 4
Spring 5
Spring 6
x1
k1
k2
k3
k4
k5
k6

## Slide 17: Example of stochastic orientation state build-up with platelets count
x1
x3
x2
Domain cumulative thickness
Domain occupied by a tensile coupon made of platelets
Chart: Stochastic orientation build-up with platelets count
| 0.04 | 0.08 | 0.12 | 0.16 | 0.2 | 0.24 | 0.32 | 0.4 | 0.6 | 0.8 | 1
 | 0.46207 | 0.47354 | 0.46328 | 0.47339 | 0.48379 | 0.49556 | 0.51327 | 0.52203 | 0.52411 | 0.5264 | 0.51987
More platelets added into the system
Domain thickness increases
More statistical probability for:
Overall platelets alignment to increase
Orientation state to be more uniform over the entire domain with fewer “weak spots” (reduced intra-coupon orientation variability)
Reduced dissimilarity (variab) of inter-coupons orientation states

## Slide 18: ambiguous relationships between morphological descriptors of a complex system
Lp= var
wp= var
tp= var
Platelet size
Stress transfer in a platelet system
Platelets count in a platelet system
Other descriptors/characteristics of system morphology
Platelet system internal redundancy
(for both stochastic and deterministic orientation states)
Variability of stochastic orientation state
Overlapping between platelets  stress sharing efficiency (stochastic & deterministic)
Platelet Size Effects on
Composite Morphology

## Slide 19: Computational modeling of progressive damage in a stochastic platelet composite system

## Slide 20: Fundamental premises for computational modeling of damaged deformation
Multi-directional discontinuous platelet composite system is modeled as continuum in (x1,x2,x3) space with sub-domains assigned local coordinate systems (1,2,3) to represent stacked misaligned platelets.
Progressive failure analysis based on stiffness reduction scheme and smeared crack approach, is a tool to model the damaged deformation
Constitutive tensor of a platelet is 3D-stress/3D-damage stiffness matrix
σ22
σ12
σ11
σ23
σ33
σ13
x1
x2
x3
Lp
1
2
1
2
wp

## Slide 21: Continuum damage mechanics based material model of a platelet
Damaged constitutive tensor:
Damage initiation criteria:
Damage evolution laws:

## Slide 22: Algorithm in image of reality: physical vs model stochastic morphology
Virtually Generated Meso-Scale Morphology
“Pseudo-Random”
True stochastic nature is approximated by an algorithm, operated on a “pseudo-random” number generation after a given probability distribution function.
  Virtual platelets are placed sequentially by generating the center points and an angle according to an orientation distribution function
Uncontrolled Stochastic Morphology
from Manufacturing

## Slide 23: demonstration
0
1
Damage index
x1
x2
x3
x1
x2
x3
0
0.4
0.8
1.2

## Slide 24: structure-property relationship in prepreg platelet systems

## Slide 25: Influential factors for composite effective properties (stochastic system)
Effect of platelet size, length (Lp) and thickness (tp)
Effect of variability of stochastic orientation state caused by platelets count:
  Scaling of composite effective properties with composite thickness (t)
Effect of the platelets alignment on tensile properties of a composite system
Lp
wp
tp
1
2
Lp= var
wp= var
tp= var
x1
x2
x3
t

## Slide 26: Platelets count (fixed platelet size) & Stochastic orientation state
Platelets Count
Fewer platelets/orientation:
  More orientation dissimilarity between volumes
  More local orientation dissimilarity within a volume
There is a limited number of platelets and orientations within a given volume
Platelet system with a stochastic orientation state
More Platelets  More Orientations
Fewer Platelets  Fewer orientations
More platelets/orient’s increases the probability of having more alignment
t1
t2 > t1

## Slide 27: Distribution of local platelets alignment as function of coupon thickness (virtual, 2D-random)
x1
x2
x3
152.4mm (6in)
25.4mm (1in)
3.6mm (0.142in)
1.0mm (0.039in)
Chart: Coupon thickness = 1mm: avg. 0.49 (cov. 5%)
 | 0.53022 | 0.47157 | 0.50325 | 0.49757 | 0.55436
 | 0.41461 | 0.39083 | 0.53943 | 0.50154 | 0.53869
 | 0.51186 | 0.52304 | 0.54602 | 0.48167 | 0.40937
 | 0.50593 | 0.40947 | 0.52304 | 0.42011 | 0.56961
 | 0.49035 | 0.44305 | 0.52381 | 0.46025 | 0.54811
 | 0.57005 | 0.44587 | 0.47104 | 0.42387 | 0.57734
Chart: Coupon thickness = 3.6mm: avg. 0.5 (cov. 0.75%)
 | 0.48611 | 0.42012 | 0.51186 | 0.50695 | 0.49853
 | 0.54935 | 0.48165 | 0.51612 | 0.51456 | 0.51022
 | 0.53159 | 0.46247 | 0.53924 | 0.48554 | 0.49801
 | 0.52028 | 0.46794 | 0.46509 | 0.49048 | 0.48434
 | 0.48269 | 0.53283 | 0.50991 | 0.50699 | 0.49876
 | 0.44254 | 0.53099 | 0.54782 | 0.52621 | 0.51946
Coupon thickness (mm) | Avg. platelets/coupon
1.0 | 337
3.6 | 949
0.5x0.5in platelets
Less intra-coupon variability of platelets alignment
Less inter-coupon variability of platelets alignment

## Slide 28: coupon thickness effect on tensile properties (stochastic system): experimental & simulated
x2
x1
x3
w
t
L
Chart: Coupon thickness, t
| (0.75-0.87)mm | 1.00 mm | (1.31-1.53)mm | 3.6 mm | 3.7mm
 | 103.4631 | 159.84 | 196.8168 | 241.88 | 222.8793
 | 96.3931 | 168.34 | 203.6669 | 253.52 | 163.1919
 | 108.6421 | 236.13 | 202.6363 | 218.88 | 195.8963
 | 117.3053 | 212.73 | 218.3005 | 259.09 | 257.9366
 | 107.4286 | 188.4 | 172.6177 | 251.28 | 179.1972
 | 105.4003 | 163.9 | 177.1451 | 216.27 | 221.0896
 | 142.7299 | 177.1588 | 138.5852 | 213.28 | 238.2979
 | 120.0323 | 136.8544 | 140.1888 | 224.79 | 260.9239
 | 112.2789 | 156.3293 | 150.2429 | 182.36 | 184.3913
 | 109.5905 | 95.8211 | 162.9739 | 203.244 | 263.0147
 | 221.9936 | 144.6975 | 303.6812 | 230.5645
 | 259.8188 | 129.5896 | 266.3253 | 228.9394
Experimental
Simulation
(3D-stress/3D-damage)
0.5x0.5in platelets

## Slide 29: Effect of increased platelet length on stiffness & strength of stochastic system
Efficiency of Stress Sharing
Platelets Length, Lp (tp=const)
Platelets Count
x1
x2
x3
Improved Performance
Increased Variability

## Slide 30: Case-study: platelet length effect on performance characteristics of a stochastic system
25.2mm (~1in)
151.9 mm (~6in)
2.5mm (0.098in)
Virtual tensile coupons of platelets / 5 individually generated (“2D-random”) and 5 extracted from a plaque (“2D-random”); Coupon thickness = 2.5mm;
Platelets: tp=0.1mm; Platelet length (Lp) is varied as 0.5in, 1.0in, 2.0in (Lp/wp=4)
Lp x wp = 50.8 x 12.7mm
(avg. 291 platelets/coupon)
Lp x wp = 25.4 x 6.35mm
(avg. 638 platelets/coupon)
Lp x wp = 12.7 x 3.175mm
(avg. 1,685 platelets/coupon)
x1
x2
x3

## Slide 31: simulated Platelet length effect on stiffness & strength in a stochastic system
Added efficiency
Increased variability
Chart: Platelet size, Lp x wp (mm)
| 12.7 x 3.175 mm | 25.4 x 6.35 mm | 50.8 x 12.7 mm
 | 39.61 | 44.282 | 48.411
 | 39.497 | 41.533 | 54.206
 | 38.933 | 45.869 | 54.755
 | 39.333 | 42.528 | 47.147
 | 38.93 | 46.638 | 54.276
 | 38.359 | 40.788 | 49.732
 | 38.187 | 39.143 | 37.109
 | 40.267 | 41.287 | 47.874
 | 38.657 | 40.401 | 45.773
 | 36.108 | 41.956 | 47.258
Chart: Platelet size, Lp x wp (mm)
| 12.7 x 3.175 mm | 25.4 x 6.35 mm | 50.8 x 12.7 mm
 | 256.6789 | 263.3266 | 296.0154
 | 217.0667 | 255.1587 | 294.7652
 | 252.4176 | 270.81 | 375.9048
 | 244.7928 | 270.2624 | 306.3699
 | 249.9905 | 289.6598 | 328.9579
 | 244.3715 | 249.7327 | 274.73
 | 224.2914 | 243.7188 | 239.186
 | 246.8853 | 274.6441 | 314.4853
 | 240.5052 | 219.4232 | 289.3227
 | 222.9497 | 269.1549 | 287.71

## Slide 32: Platelet length-to-thickness ratio & efficiency of stress transfer (stochastic system)
Chart: Platelet length, Lp=12.7mm, Lp/wp=4
| 0.2mm / 5.0mm | 0.1mm / 2.5mm | 0.05mm / 1.25mm
 | 35.55 | 39.61 | 42.749
 | 35.446 | 39.497 | 42.598
 | 34.936 | 38.933 | 41.992
 | 35.231 | 39.333 | 42.466
 | 34.924 | 38.93 | 42.021
Chart: Platelet thickness, tp (mm) / Tensile bar thickness (mm)
| 0.2mm / 5.0mm | 0.1mm / 2.5mm | 0.05mm / 1.25mm
 | 205.8677 | 256.6789 | 300.9677
 | 181.7718 | 217.0667 | 268.3595
 | 205.1996 | 252.4176 | 308.4173
 | 196.8226 | 244.7928 | 289.3522
 | 200.1918 | 249.9905 | 302.7025
“Shrinking”/”swelling” a virtual coupon with preserved morphology by varying platelet thickness
Morphology variability effect on composite stiffness/strength from platelet size effect is separated. Increased platelet length-to-thickness ratio is responsible for improved composite properties

## Slide 33: Effect of using thinner platelets (thinner tape): concept
2.5mm-thick tensile coupons;
Lp=2in (Lp/wp=4);
Platelet thickness (tp) :
  tp= 0.050 mm
  tp= 0.100 mm
  tp= 0.250 mm
Virtual tensile coupons were individually generated by 2D-random orientation tensor
Stress Transfer Efficiency
Platelets Count
Platelet Thickness
t=10(tp);
tp=250μm
t=25(tp);
tp=100μm
t=50(tp);
tp=50μm

## Slide 34: Effect of using thinner platelets (thinner tape): analysis results
Chart: Platelet thickness, tp (mm)
| 0.05 | 0.1 | 0.25
 | 49.709 | 48.411 | 46.188
 | 53.015 | 54.206 | 49.601
 | 52.998 | 54.755 | 46.497
 | 53.466 | 47.147 | 44.941
 | 51.398 | 54.276 | 42.155
Chart: Platelet thickness, tp (mm)
| 0.05 | 0.1 | 0.25
 | 384.1367 | 296.0154 | 193.3583
 | 408.5109 | 294.7652 | 262.805
 | 404.6954 | 375.9048 | 244.9311
 | 404.556 | 306.3699 | 213.9862
 | 418.8333 | 328.9579 | 158.2315
Added efficiency
Reduced variability
Thicker platelets
Thinner platelets

## Slide 35: Effect of platelets alignment on effective tensile properties: experimental (narrow platelet)
1.5-mm thick tensile coupons with enhanced alignment were manufactured, platelet in-plane angle = -10°..10°
Chart: Coupon thickness, t
| ROS~0.6mm | ROS~1.55mm | ROS~3.7mm | EA~1.5mm
 | 26003 | 35077 | 40725
 | 29083 | 33473 | 37900
 | 31550 | 36684 | 34887
 | 25433 | 37752 | 37230
 | 22679 | 43120 | 40328
 | 26313 | 29685 | 45152.05
 | 22557 | 35907 | 43425.51
 | 21669 | 48853 | 38258.99
 | 29674 | 30310 | 36349.62
 | 27097 | 45414 | 35707.04 | 83833
 | 48051 | 92105
 | 43814 | 93633
Chart: Coupon thickness, t
| ROS~0.55mm | ROS~1.55mm | ROS~3.7mm | EA~1.5mm
 | 92.48 | 118.24 | 239.96
 | 91.36 | 122.77 | 209.73
 | 75.88 | 140.64 | 274.7
 | 99.44 | 148.8 | 333.92
 | 89.79 | 191.74 | 334.01
 | 84.76 | 162.99 | 283.2917
 | 69.75 | 172.75 | 216.7876
 | 65.49 | 205.42 | 302.8308
 | 74.85 | 150.82 | 297.9537
 | 102 | 158.77 | 267.5334
 | 316.1562
 | 251.6727
x1
x2
x3
x1
x2
x3
Enhanced Alignment
w
t
L

## Slide 36: improved performance with increased platelets alignment (stochastic system): analysis
Chart: platelet: Lp x wp = 12.7 x 12.7mm; tp=0.1mm; bar: L=6'', w=1''
| 0.248198 | 0.24024000000000001 | 0.259963 | 0.24493300000000001 | 0.24857699999999999 | 0.36368200000000001 | 0.34248600000000001 | 0.35263800000000001 | 0.35878599999999999 | 0.34364699999999998 | 0.45893299999999998 | 0.44509300000000002 | 0.44232500000000002 | 0.41368199999999999 | 0.44469999999999998 | 0.50049500000000002 | 0.49456499999999998 | 0.50095100000000004 | 0.50373599999999996 | 0.50837900000000003 | 0.57449600000000001 | 0.54654899999999995 | 0.56155900000000003 | 0.55928999999999995 | 0.55981700000000001 | 0.631552 | 0.654308 | 0.66176000000000001 | 0.66739700000000002 | 0.64385099999999995 | 0.75271699999999997 | 0.759459 | 0.76705699999999999 | 0.77127699999999999 | 0.76622000000000001
simulated results, t=3.6mm | 22.236 | 19.409 | 22.284 | 21.253 | 22.569 | 27.297 | 27.19 | 29.729 | 29.222 | 27.366 | 37.973 | 36.523 | 37.031 | 32.251 | 35.502 | 41.535 | 40.441 | 43.146 | 42.256 | 42.003 | 47.804 | 47.706 | 47.241 | 47.385 | 46.376 | 55.839 | 58.237 | 61.261 | 62.148 | 56.634 | 72.766 | 74.497 | 73.948 | 77.249 | 73.679
experim QLF 0499683b | 37.115 | 38.736 | 41.954 | 38.13 | 40.692
experim QHF 0498903,05,06,07 | 50.1 | 57.3 | 59.4 | 57.9
Chart: Degree of platelets alignment with loading direction, a11
| 0.248198 | 0.24024000000000001 | 0.259963 | 0.24493300000000001 | 0.24857699999999999 | 0.36368200000000001 | 0.34248600000000001 | 0.35263800000000001 | 0.35878599999999999 | 0.34364699999999998 | 0.45893299999999998 | 0.44509300000000002 | 0.44232500000000002 | 0.41368199999999999 | 0.44469999999999998 | 0.50049500000000002 | 0.49456499999999998 | 0.50095100000000004 | 0.50373599999999996 | 0.50837900000000003 | 0.57449600000000001 | 0.54654899999999995 | 0.56155900000000003 | 0.55928999999999995 | 0.55981700000000001 | 0.631552 | 0.654308 | 0.66176000000000001 | 0.66739700000000002 | 0.64385099999999995 | 0.75271699999999997 | 0.759459 | 0.76705699999999999 | 0.77127699999999999 | 0.76622000000000001
t=3.6mm (simulated results) | 121.2004 | 114.1847 | 128.5618 | 94.723 | 138.2773 | 175.0647 | 133.0191 | 160.5638 | 157.4729 | 146.0554 | 216.2715 | 213.2754 | 224.7948 | 182.3564 | 203.244 | 241.8842 | 253.5187 | 218.8822 | 259.0858 | 251.2757 | 303.6812 | 266.3253 | 297.8675 | 256.033 | 247.6613 | 324.4063 | 363.1543 | 353.1979 | 400.6749 | 345.204 | 392.661 | 428.0851 | 461.32 | 479.4323 | 437.0629
experim QLF 0499683b | 221.09 | 238.3 | 260.92 | 184.39 | 263.01
experim QHF 0498903,05,06,07 | 292 | 326.8948 | 438.0528 | 386.056
x1
x2
x3
x1
x2
x3
x1
x2
Degree of platelets alignment, a11

## Slide 37: Modeled variability from virtual characterization (stochastic system)
Global (all coupon) a11= 0.45 – 0.55
Enforcing inter-coupon variability of orientation state by modifying the global degree of alignment allows to more realistically model the morphology caused effective composite properties
Chart: 1/2x1/2in platelets; bar thickn=3.6mm
| Simulation | Experimental
 | 41.492 | 44.226
 | 40.46 | 39.073
 | 43.109 | 36.631
 | 42.223 | 40.757
 | 41.975 | 35.395
 | 37.924 | 37.115
 | 36.464 | 38.736
 | 36.959 | 41.954
 | 32.194 | 38.13
 | 35.494 | 40.692
 | 47.798 | 39.872
 | 47.698 | 42.262
Chart: 1/2x1/2in platelets; bar thickn=3.6mm
| Simulation | Experimental
 | 241.88 | 222.8793
 | 253.52 | 163.1919
 | 218.88 | 195.8963
 | 259.09 | 257.9366
 | 251.28 | 179.1972
 | 216.27 | 221.0896
 | 213.28 | 238.2979
 | 224.79 | 260.9239
 | 182.36 | 184.3913
 | 203.244 | 263.0147
 | 303.6812 | 230.5645
 | 266.3253 | 228.9394

## Slide 38: Main observations in prepreg platelet systems with stochastic orientation state
The strength of a composite increases with platelet length for a constant thickness (of tape and tensile coupon)
Longer platelets provide for increased variability in effective properties
Thinner tape provides for reduced variability and increased averages of effective properties
Effective properties depend on coupon thickness
Lp
wp
tp
1
2
x1
x2
x3
t
Supported by experimental observations of different research groups